Data/hora: 02/06/2024 02:57:20

Provedor de dados: 	Institutional Archive of Ifreme (ArchiMer)	
País: 	France	
Título: 	Influence of dissolved oxygen content on the bacteria‐induced ennoblement of stainless steels in seawater and its consequence on the localized corrosion risk	
Autores: 	Trigodet, Florian; Larché, Nicolas; Morrison, Hilary G.; Maignien, Lois; Thierry, Dominique.	
Data: 	2019-12	
Ano: 	2019	
Palavras-chave: 	16S rRNA gene; Electroactive bacteria; Ennoblement; Microbial ecology; Natural seawater; Stainless steel.	
Resumo: 	The ennoblement of stainless steel (e.g., the increase of open circuit potential [OCP]) is associated with bacterial colonization. This increases the risk of localized corrosion as the critical pitting/crevice potential can be overcome, especially for lower grade stainless steel. In this study, we assessed the influence of dissolved oxygen content (DOC) on the crevice corrosion of duplex and super duplex stainless steels. In addition, we used DNA amplicon sequencing to identify the bacteria most likely associated with the ennoblement. Above approximately 100 parts per billion (ppb) of dissolved oxygen, the ennoblement of OCP was observed leading to an increased risk of localized corrosion. Below approximately 100 ppb of dissolved oxygen, no ennoblement occurred and the risk of localized corrosion was reduced. We identified certain hydrocarbon‐degrading bacteria whose presence correlated with the ennoblement of super duplex stainless steel at saturated DOC. The role of these bacteria is not clear yet, but their distribution indicates a possible involvement in stainless steel ennoblement in seawater.	
Tipo: 	Text	
Idioma: 	Inglês	
Identificador: 	https://archimer.ifremer.fr/doc/00588/70026/67934.pdf

DOI:10.1002/maco.201911225

https://archimer.ifremer.fr/doc/00588/70026/	
Editor: 	Wiley	
Formato: 	application/pdf	
Fonte: 	Materials And Corrosion-werkstoffe Und Korrosion (0947-5117) (Wiley), 2019-12 , Vol. 70 , N. 12 , P. 2238-2246	
Fonte: 	info:eu-repo/semantics/openAccess

restricted use