Data/hora: 05/06/2024 13:22:57

Provedor de dados: 	45	
País: 	Brazil	
Título: 	Epoxy putty external skeletal fixation in a tibiotarsal fracture of a wild choroy parakeet (Enicognathus leptorhynchus)	
Autores: 	Arias,J. I.; Beato,C.; Espinoza,A.	
Data: 	2015-06-01	
Ano: 	2015	
Palavras-chave: 	Parakeet; Epoxy putty; External skeletal fixation; Tibiotarsal fracture.	
Resumo: 	Tibiotarsal fractures are common in birds because in most birds this is the longest, most exposed bone in the leg. Transverse fractures are most common and rotational and shear forces must be stabilized in order to achieve good bone regeneration. A 230g male Slender-billed Parakeet or Choroy parakeet (Enicognathus leptorhynchus), with more than five years of age, was received with non-weight bearing lameness with 24 hours duration. X-rays were taken, and these revealed a closed, complete, non-comminuted transverse fracture of the distal diaphysis of the left tibiotarsal bone. Fixation was planned with 10-minute fast-setting epoxy putty. In order to assess the temperature of polymerization of the epoxy dough and the possibility of heat-bone necrosis, the temperature was recorded every 30 seconds for 12 minutes with three different amounts of the epoxy material in an ex vivo test. The temperature of the pieces reached a peak of 50-60ºC, where the highest peak corresponds to the highest amount of material. When approximately 6g of putty were used, the peak temperature reached only 51ºC. This peak changed to 58ºC when 4 times more epoxy was mixed and measured. If the temperature of the pins inserted in the bone exceeds 70ºC, bone necrosis could occur. In light of these results, the fracture was treated with 6 g of epoxy putty that was allowed to polymerize over a 1A 2/2 external skeletal fixation, with 1-mm pins bent at 90º and joined together with cerclage wire. At 6 weeks after surgery the bird had formed a good primary bone callus, and the external fixators were therefore removed. With this approach a satisfactory recovery of the patient was achieved with normal use of the affected limb.	
Tipo: 	Info:eu-repo/semantics/article	
Idioma: 	Inglês	
Identificador: 	http://www.scielo.br/scielo.php?script=sci_arttext&pid=S0102-09352015000300671	
Editor: 	Universidade Federal de Minas Gerais, Escola de Veterinária	
Relação: 	10.1590/1678-4162-7474	
Formato: 	text/html	
Fonte: 	Arquivo Brasileiro de Medicina Veterinária e Zootecnia  v.67 n.3 2015	
Fonte: 	info:eu-repo/semantics/openAccess